## Slide 1
Juan Bian, Yun Xue, Kai Yao, Xue Gu, Chao Yan, Yan Wang
School of Pharmacy, Shanghai Jiao Tong University, Shanghai 200240, China
Rovshen Charygeldiyev
Vrije University Amsterdam
Solid-phase extraction approach for phospholipids profiling by titania-coated silica microspheres prior to reversed-phase liquid chromatography–evaporative light scattering detection and tandem mass spectrometry analysis
Talanta. 2014 Jun;123:233-40. doi: 10.1016/j.talanta.2014.02.001. Epub 2014 Feb 12.

## Slide 2: Stationery phase of SPE column for phospholipids extraction
Type of SPE column | Advantages | Disadvantages
Porous Si, Si modified with C18, CN, NH2 groups |  | Not high selectivity and efficiency
Metal oxides (ZrO2, TiO2) | Higher selectivity (binding affinity for phosphate groups) | Small surface area, pore volume, lack of porous structure
Metal oxide-coated mesoporous silica | Large surface area Large pore volume Highly selective and efficient isolation | 
Synthesis: water-vapor-induced internal hydrolysis:
  Tetrabutyl titanate (Ti(OC4H9)4) + Silica microspheres
Synthesized material: employed as a sorbent in SPE column

## Slide 3
XRD spectra of the SiO2, TiO2, 5 wt% TiO2/SiO2, 7.5 wt% TiO2/SiO2 and 10 wt% TiO2/SiO2.
No peaks corresponding to crystalline TiO2 – all TiO2 on surface of SiO2

## Slide 4
The BET surface areas
SiO2 (m2/g) | 346.9385
10 wt% SiO2/TiO2 | 338.2478
7,5 wt% SiO2/TiO2 | 341.1507
5 wt% SiO2/TiO2 | 335.8712
TiO2 | 36.1042
Slight difference between pure SiO2 and SiO2/TiO2 - means surface area is sufficient
Pore size distribution curve from BJH adsorption
Average pore size for both SiO2 and SiO2/TiO2 materials: 12 nm

## Slide 5
SPE-LS – loading solution;
SPE-WS – washing solution;
SPE-ES – eluting solution
RPLC-ELSD | 
Column | C8 4.6 mm i.d.x250 mm; 5 μm particle size
Mobile phase | 10 mmol/LAA-ammonium acetate in MeOH
Flow rate | 1 mL/min
Gradient conditions | 0-15 min, 50-100% B; 15-30 min, 100% B
Temperature | 45°C
Effluents free of PLs
Clean PLs in eluting solution

## Slide 6
Extracted ion chromatograms from UPLC–QTOF MS in positive ion mode
UPLC–QTOF MS | 
Column | C8 2.1 mm i.d.x100 mm; 1,7 μm particle size
Mobile phase | 10 mmol/L ammonium formate in ACN/water (A) 10 mmol/L ammonium formate in MeOH (B)
Flow rate | 0,4 mL/min
Temperature | 45°C